Certificate of Analysis

General properties:

Name：NHS-PEG3400-PLA2000

Molecular Weight： 5500 Dalton

Cat.#： R-P-103002

Lot.#： RP201605006

Manufacture Date： 2016.05.06

Date of Analysis： 2016.05.06

Recommended Retest date： 2017.05.06

Stability： 12 months

Storage： -20°C in the dark

Structure

| Items | Specification | Results |
| --- | --- | --- |
| Appearance | White/ Light yellow solid | White solid |
| 1H NMR | Identical to the Structure | Identical to the Structure |
| Foreign Material | None | None |
| Substitution | ＞90% | 93% |
| PDI |  | <1.4 |

Report Date: 2016.05.06

核磁图谱：

This product is for research use only, Not for human or animal use