Certificate of Analysis

General properties:

Name： PEG3400-S-S-PDLLA5000

Molecular Weight： PEG MW:3400, PDLLA MW:5000

Cat.#： RQD10020

Lot.#： RP0162067

Manufacture Date： 2016.06.20

Date of Analysis： 2016.06.20

Recommended Retest date： 2017.06.20

Stability： 12 months

Storage： -20°C in the dark

Structure

| Items | Specification | Results |
| --- | --- | --- |
| Appearance | White/ Light yellow solid | Light yellow solid |
| 1H NMR | Identical to the structure | Identical to the structure |
| Foreign Material | None | None |
| Substitution | ＞90% | 93% |
| PDI |  | ＜1.3 |

Report Date: 2016.06.20

This product is for research use only, Not for human or animal use