Certificate of Analysis

General properties:

Name：MAL-PEG3400-PLA2000，(PLA,DL型)

Molecular Weight： PEG, MW:3400  PLA,MW:2000

Cat.#： R-D-12002

Lot.#： 854515

Manufacture Date： 2016.01.20

Date of Analysis： 2016.01.20

Recommended Retest date： 2017.01.20

Stability： 12 months

Storage： -20°C in the dark

Structure

| Items | Specification | Results |
| --- | --- | --- |
| Appearance | White/ Off-white solid | White solid |
| 1H NMR | Identical to the structure | Identical to the structure |
| Foreign Material | None | None |
| Substitution | ＞90% | 91% |

Report Date: 2016.01.20

核磁图谱：

This product is for research use only, Not for human or animal use