Certificate of Analysis

General properties:

Name：Gold Nanoparticles；Colloidal gold (50nm)

CAS ：7440-57-5

Cat.#：R-J5005

Lot.#：RJ201604005

Manufacture Date：2016.04.05

Date of Analysis：2016.04.05

Recommended Retest date： 2016.10.05

Stability：6 months

Storage：4℃

| Items | Specification | Results |
| --- | --- | --- |
| Appearance | Wine red solution | Wine red solution |
| Foreign Material | None | None |
| Concentration | 48.26μg/ml | 48.26μg/ml |
| Size | 50nm | 46-50nm |
| Dispersant | H2O | H2O |

Report Date: 2016.04.05

This product is for research use only, Not for human or animal use