Certificate of Analysis

General properties:

Name： Alkyne-PEG2000-NH2

Molecular Weight:  2000Dalton

Cat.#:  R-9901

Lot.#:  AN160120

Manufacture Date:  2016.01.20

Date of Analysis:  2016.01.20

Recommended Retest date:  2017.01.20

Stability:  12 months

Storage:  -20°C in the dark

Structure

| Items | Specification | Results |
| --- | --- | --- |
| Appearance | White/ Off-white solid | White solid |
| 1H NMR | Identical to the Structure | Identical to the Structure |
| Foreign Material | None | None |
| Substitution | ＞90% | 90% |

Report Date: 2016.01.20

This product is for research use only, Not for human or animal use