Certificate of Analysis

General properties:

Name： HO-PEG5000-COOH

Molecular Weight： 5000 Dalton

Cat.#：R-1049

Lot.#：1509511

Manufacture Date： 2015.08.13

Date of Analysis： 2015.08.13

Recommended Retest date： 2016.08.13

Stability： 12 months

Storage： -20°C in the dark

Structure

| Items | Specification | Results |
| --- | --- | --- |
| Appearance | White/ Off-white solid | White solid |
| 1H NMR | Identical to the Structure | Identical to the Structure |
| Foreign Material | None | None |
| Purity | ＞90% | 90% |

Report Date: 2015.08.13

This product is for research use only, Not for human or animal use