Certificate of Analysis

General properties:

Name：MAL-PEG2000-OH

Molecular Weight： 2000 Dalton

Cat.#： R-1074

Lot.#： 685451

Manufacture Date： 2015.12.09

Date of Analysis： 2015.12.09

Recommended Retest date： 2016.12.09

Stability： 12 months

Storage： -20°C in the dark

Structure

| Items | Specification | Results |
| --- | --- | --- |
| Appearance | Light yellow/ yellow solid | Light yellow solid |
| 1H NMR | Identical to the structure | Identical to the structure |
| Foreign Material | None | None |
| Substitution | ＞90% | 90% |

Report Date: 2015.12.09

This product is for research use only, Not for human or animal use