西安瑞禧生物科技有限公司

Certificate of Analysis

General properties:

Name： NH2-PEG2000-NH2

Molecular Weight:  2000Dalton

Cat.#:  R-1037

Lot.#:  558841

Manufacture Date:  2015.10.30

Date of Analysis:  2015.10.30

Recommended Retest date:  2016.10.30

Stability:  12 months

Storage:  2-8°C in the dark

Structure

| Items | Specification | Results |
| --- | --- | --- |
| Appearance | White/off-white solid | White solid |
| 1H NMR | Identical to the Structure | Identical to the Structure |
| Foreign Material | None | None |
| Substitution | ＞90% | 90% |

Report Date: 2015.10.30

This product is for research use only, Not for human or animal use

Xi'an ruixi Biological Technology Co., Ltd                              Web:http://www.xarxbio.com

Xi'an city ,Shaanxi Province, China                                      http://www.resenbio.com

Tel: 0086 29 86354885                                               E-mail:sales@xarxbio.com